10 things to check for GMAW

- Check equipment

- Turn CO 2 tank all the way on and set psi to 25

- Set to DC-

- Set ground clamp

- Set wirefeed to 35

- Set voltage range to 5

- Clean nozzle and tip

- Cut wire 1/8” stick out

- Gun angle should be 90 & 25

- 10 second per inch